Tarasafe Super

TARASAFE SUPER is a slip resistant safety vinyl floorcovering, with a vinyl wear layer and deeply inlaid mineral crystal particles (patented).

It is reinforced by a glass fibre grid and available in a sheet format. It is an ideal solution for heavy traffic applications where slip resistance, durability, hygiene and easy maintenance are required.

According to ISO 22196, it has anti bacterial activity against MRSA of 99% after 24h00.

TARASAFE SUPER is suitable for most contract & commercial areas. It is eco-friendly, 100% recyclable, Floorscore® certified and does not contain any heavy metals or CMR 1&2, it is also 100% compliant with REACH.

The product emission rate of volatile organic compounds is < 100 µg/m3 (TVOC after 28 days – ISO 16000 -6).